## Slide 1: T0TEM – T0 Test Evaluation Module
ASTM Committee Week 11/6/2018
ASTM E08.07.06 – E1921
Levi Shelton
Cameron Bosley
National Aeronautics and Space Administration
www.nasa.gov

## Slide 2: Topics
Status
Software Overview
Testing Results
Planned Additions
Working Group Distribution

## Slide 3: Status
Basic functionality complete:
  Standard T0 calculation (multi-temp and single temp methods)
  Master Curve plotting and selectable confidence bounds
  Bi-modal and multi-modal calculations and plots
  US and SI unit selectable
  Manual entry/file select input
  Margin adjustment
Work still being done on:
  Output Files
  Input File formatting

## Slide 4: Software Overview

## Slide 5: Software Overview

## Slide 6: Software Overview

## Slide 7: Software Overview

## Slide 8: Software Overview

## Slide 9: Software Overview

## Slide 10: Testing Results
For E1921 example problem:
  Time to calculate standard T0 <5s
  Time to calculate inhomogeneity results <5s
  T0TEM has non-significant differences (<0.3%) from standard results

## Slide 11: Testing Results: Bi-Modal
 |  |  |  |  |  |  |  |  |  | Absolute Diff |  | Percent Diff | 
 |  | Standard |  |  |  | T0TEM |  |  |  | T0TEM/Standard |  | T0TEM/Standard | 
Ti – To | Ti | KA(T) | KB(T) | KJc(0.05) | KJc(0.95) | KA(T) | KB(T) | KJc(0.05) | KJc(0.95) | KJc(0.05) | KJc(0.95) | KJc(0.05) | KJc(0.95)
(oC) | (oC) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m)
-50 | -98 | 53.6 | 67.1 | 37.7 | 77.1 | 53.6 | 67.1 | 37.7 | 77.1 | -0.01 | 0.04 | -0.03 | 0.05
-45 | -93 | 55.9 | 70.7 | 38.9 | 81.5 | 55.9 | 70.7 | 38.9 | 81.5 | 0.00 | 0.00 | 0.01 | 0.00
-40 | -88 | 58.4 | 74.6 | 40.2 | 86.3 | 58.4 | 74.6 | 40.2 | 86.3 | 0.04 | 0.00 | 0.10 | 0.00
-35 | -83 | 61.1 | 79 | 41.7 | 91.6 | 61.1 | 79.0 | 41.7 | 91.6 | 0.01 | -0.02 | 0.03 | -0.02
-30 | -78 | 64.1 | 83.7 | 43.3 | 97.4 | 64.1 | 83.8 | 43.3 | 97.4 | 0.03 | -0.01 | 0.06 | -0.01
-25 | -73 | 67.4 | 89 | 45.1 | 103.8 | 67.4 | 89.0 | 45.1 | 103.8 | 0.00 | -0.03 | 0.00 | -0.03
-20 | -68 | 71.1 | 94.8 | 47.1 | 110.8 | 71.1 | 94.8 | 47.1 | 110.8 | -0.05 | -0.01 | -0.10 | -0.01
-15 | -63 | 75.1 | 101.2 | 49.2 | 118.5 | 75.1 | 101.2 | 49.2 | 118.5 | 0.00 | 0.01 | -0.01 | 0.01
-10 | -58 | 79.4 | 108.2 | 51.6 | 127 | 79.5 | 108.2 | 51.6 | 127.0 | -0.04 | 0.01 | -0.09 | 0.00
-5 | -53 | 84.3 | 115.8 | 54.1 | 136.3 | 84.3 | 115.9 | 54.1 | 136.3 | 0.05 | 0.04 | 0.09 | 0.03
0 | -48 | 89.6 | 124.3 | 57 | 146.6 | 89.6 | 124.3 | 57.0 | 146.6 | 0.00 | 0.01 | 0.00 | 0.01
5 | -43 | 95.4 | 133.6 | 60.1 | 157.9 | 95.4 | 133.6 | 60.1 | 157.9 | 0.03 | 0.00 | 0.05 | 0.00
10 | -38 | 101.9 | 143.8 | 63.6 | 170.3 | 101.9 | 143.8 | 63.6 | 170.3 | -0.02 | 0.02 | -0.04 | 0.01
15 | -33 | 108.9 | 155.1 | 67.4 | 184 | 108.9 | 155.1 | 67.4 | 184.0 | -0.04 | -0.03 | -0.05 | -0.01
20 | -28 | 116.7 | 167.5 | 71.5 | 199 | 116.7 | 167.5 | 71.5 | 199.0 | 0.03 | -0.01 | 0.04 | 0.00
25 | -23 | 125.2 | 181.1 | 76.1 | 215.5 | 125.3 | 181.1 | 76.1 | 215.5 | 0.01 | 0.00 | 0.01 | 0.00
30 | -18 | 134.6 | 196 | 81.1 | 233.7 | 134.7 | 196.0 | 81.1 | 233.7 | 0.05 | -0.04 | 0.06 | -0.02
35 | -13 | 145 | 212.5 | 86.7 | 253.6 | 145.0 | 212.5 | 86.7 | 253.6 | -0.02 | 0.03 | -0.02 | 0.01
40 | -8 | 156.3 | 230.6 | 92.8 | 275.6 | 156.4 | 230.6 | 92.8 | 275.6 | -0.03 | -0.02 | -0.03 | -0.01
45 | -3 | 168.8 | 250.4 | 99.5 | 299.7 | 168.9 | 250.5 | 99.5 | 299.7 | -0.03 | 0.03 | -0.03 | 0.01
50 | 2 | 182.6 | 272.3 | 106.8 | 326.3 | 182.6 | 272.3 | 106.8 | 326.3 | 0.03 | -0.02 | 0.03 | -0.01

## Slide 12: Testing Results: Multi-Modal
 |  |  |  |  |  |  |  | Percent Diff |  | 
 |  | Standard |  |  | T0TEM |  |  | T0TEM/Standard |  | 
Ti – Tm | Ti | KJc(0.50) | KJc(0.05) | KJc(0.95) | KJc(0.50) | KJc(0.05) | KJc(0.95) | KJc(0.50) | KJc(0.05) | KJc(0.95)
(oC) | (oC) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m) | (MPa√m)
-51 | -95 | 56.24 | 38.11 | 79.50 | 56.24 | 38.11 | 79.50 | 0.00 | 0.01 | 0.01
-46 | -90 | 58.83 | 39.35 | 84.09 | 58.83 | 39.35 | 84.10 | -0.01 | -0.01 | 0.01
-41 | -85 | 61.69 | 40.72 | 89.16 | 61.69 | 40.72 | 89.16 | 0.01 | 0.00 | 0.01
-36 | -80 | 64.82 | 42.23 | 94.72 | 64.83 | 42.23 | 94.72 | 0.01 | 0.01 | 0.00
-31 | -75 | 68.27 | 43.88 | 100.85 | 68.28 | 43.88 | 100.85 | 0.01 | 0.01 | 0.00
-26 | -70 | 72.07 | 45.69 | 107.58 | 72.07 | 45.69 | 107.58 | 0.00 | 0.00 | 0.00
-21 | -65 | 76.24 | 47.68 | 114.99 | 76.24 | 47.68 | 115.00 | 0.00 | -0.01 | 0.01
-16 | -60 | 80.83 | 49.87 | 123.15 | 80.83 | 49.88 | 123.15 | 0.00 | 0.01 | 0.00
-11 | -55 | 85.87 | 52.28 | 132.11 | 85.87 | 52.28 | 132.11 | 0.00 | 0.00 | 0.00
-6 | -50 | 91.42 | 54.93 | 141.97 | 91.42 | 54.93 | 141.97 | 0.00 | 0.01 | 0.00
-1 | -45 | 97.52 | 57.83 | 152.82 | 97.52 | 57.83 | 152.82 | 0.00 | 0.00 | 0.00
4 | -40 | 104.23 | 61.03 | 164.74 | 104.23 | 61.03 | 164.74 | 0.00 | 0.00 | 0.00
9 | -35 | 111.60 | 64.54 | 177.86 | 111.61 | 64.54 | 177.86 | 0.01 | 0.00 | 0.00
14 | -30 | 119.71 | 68.40 | 192.28 | 119.72 | 68.40 | 192.29 | 0.00 | 0.00 | 0.00
19 | -25 | 128.64 | 72.64 | 208.15 | 128.64 | 72.65 | 208.15 | 0.00 | 0.01 | 0.00
24 | -20 | 138.44 | 77.31 | 225.59 | 138.45 | 77.31 | 225.60 | 0.00 | 0.00 | 0.00
29 | -15 | 149.23 | 82.44 | 244.78 | 149.24 | 82.44 | 244.78 | 0.01 | 0.00 | 0.00
34 | -10 | 161.09 | 88.08 | 265.88 | 161.10 | 88.08 | 265.88 | 0.00 | 0.00 | 0.00
39 | -5 | 174.14 | 94.28 | 289.08 | 174.14 | 94.29 | 289.08 | 0.00 | 0.01 | 0.00
44 | 0 | 188.48 | 101.10 | 314.59 | 188.49 | 101.11 | 314.60 | 0.00 | 0.01 | 0.00

## Slide 13: Planned Additions
Allow for active adjustment of plot area
Simple upper shelf plotting ability
Add list of where specimens fall into validity requirements (to help adjust temperature while testing still being conducted)
Tutorial auto runs ASTM sample set
Output of Kjc▲a and Kjc limit values
Compressing code into functions for ease of troubleshooting and operation speed
Combining standard T0 and Inhomogeneity plots

## Slide 14: Beta Testing
Following the NASA process for releasing programs. As part of that process we will provide a targeted intergovernmental release to select individuals to allow for beta testing that will ultimately be used to support a wider release.
In short term if anyone has non-sensitive/normalized data they are willing to share or would like analyzed we can send the input format file and return results for comparison.

## Slide 15: SignOffPage
Notes: NASA Presentation Sign-Off Page

## Slide 16: Demonstration